## Slide 1: Double-Clad Erbium-Ytterbium Co-Doped Fiber Laser
Matt Ruby & Colin Diehl

## Slide 2
Single-mode Fiber
High Beam Quality
Low Propagation Loss
Lower Power Pump
Expensive
Multimode Fiber
Higher Power Pump
Inexpensive
Poor Beam Quality
High Propagation Loss

## Slide 3: Types of Double-Clad Fiber

## Slide 4: Our Double-Clad Fiber

## Slide 5: Our Double-Clad Fiber
Type: Centered Core
Specs:
  Core Diameter 6µm
  First Cladding 124µm
  Second Cladding 240µm, polymer coating
Reasons of Centered Core Fiber
  Compatible with smf-28
  Easy to connectorize with current tools

## Slide 6: Laser Construction

## Slide 7: Arduino Control Circuit

## Slide 8: Box Layout

## Slide 9: Development
Initial problem
  Huge power loss with MM FC/APC to DC FC/APC
  Unknown 2nd cladding
Findings
  FC coupler took the 2nd cladding of therefore the epoxy acted as the 2nd cladding
Solution
  Used a MM 3x1 coupler to avoid using FC couplers

## Slide 10: Development
Second Problem
  Fusion splices burnt out of their splice protectors
Findings
  The hot glue that the protectors used coupled light out of the fiber, just like the FC epoxy
Solution
  We used a 1mm dia metal tube to protect the bare part of the spliced fiber, and put the protector over the tube; so the hot glue only touched the coating of the fiber

## Slide 11: Double-Clad Fiber Mode Structure
Fiber Modes
  Radial
  Azimuthal
Problem
  Radial mode suppressed in Pump beam by the fiber core
Solution
  Use mode-scrambling techniques to redistribute modes.

## Slide 13: Pump Vs Output
Findings
  We assume that the power loss after 7.1 W pump is created from thermal losses or Stimulated Brillouin scattering (SBS)

## Slide 15: SBS
Phonon photon scattering
  Thermal effects
  Signal effects
How to Observe
  SBS is a reverse propagating wave
  SBS has an intrinsic frequency shift of 10 – 20 MHz(3)

## Slide 16: Future Work
Test for SBS
  Use a 2X2 output coupler to take the back reflected light out of the cavity, then measure frequency relative to the lasers output frequency.
Optimization
  Add a second MM WDM to dump the 980nm light out of the system
  Alter EYDF length
  Try different output couplers

## Slide 17: References
Fig 1 http://en.wikipedia.org/wiki/File:Singlemode_fibre_structure.svg
Fig 2: http://en.wikipedia.org/wiki/File:OfsetDCF.png
(3) http://www.rp-photonics.com/brillouin_scattering.html